Dazzling Mystere

Pattern Series MCD2211-MCD2215

Physical Properties:

22.5” Vertical Repeat					Width:  52” (Not Available 27”)

50 1/2” Horizontal Repeat 				Total Weight (oz./sq.yd):  13.0 oz.

Drop, Non-Reversible					Total Weight (oz./lin. Yd): 20.0 oz.

20 oz Mylar Wallcovering				Fabric Type: Non-woven

Pompeii Emboss					Backing Fabric Weight: 1.8oz./sq.yard

Average Total Thickness:  16 mils

Federal Specifications:

- This wallcovering meets or exceeds all requirements of G.S.A. Federal Specification

CCC-W-408D for Type II material.

Fire Hazard Classification Results:

Tested in accordance with ASTM E-84 Tunnel Test		Flame Spread:  	Class A Pass

Class A Fire Rated						Smoke Developed:  	Class A Pass

Order Requirements:

15 yard minimum

Sold in 15 yard increments

Customs - Available upon request

Vinyl wallcovering has little or no moisture permeability. If the design, construction or maintenance of a building and/or other circumstances allows moisture to accumulate in a wall or wall cavity, vinyl wallcovering can act as a vapor barrier restricting the escape of moisture and increasing the risk of mold growth. Mold and mildew are naturally occurring and are present everywhere in nature. They need only water and organic material [such as wood, paper or plant material] to feed upon and grow. Vinyl wallcovering permeability can be increased through perforation and alternative product constructions with varying degrees of increased permeability depending on the methods used. No wallsurfacing material will prevent mold growth, however, if moisture accumulation is permitted to occur. An experienced professional who is familiar with building conditions and circumstances should be consulted concerning benefits and limitations of vinyl wallcovering

NOTE:  The assigned numerical reading and other tests referenced in this text are not intended to reflect hazards presented by this or any other material under actual fire cognitions. Consult an architect or fire safety engineer for information on applicable building codes and reduction of fire hazards, including the use of sprinklers.

Design Copyright © York Contract								6/2015