Factory

Pattern Series MRE1270-MRE1274

Installation:  *Reversible / Random Match

*every other strip optional

Width:          36” Natural Cork Wallcovering

Roll Length: 4 linear yards per single roll / 8 linear yards per double roll

Packaged:   Double Rolls

Backing:      Paper

Fire Hazard Classification Results:

Class A Fire Rated: 	ASTM E-84 Tunnel Test

Flame Spread:  	Pass

Smoke Developed:  	Pass

Notable Facts:

●  These cork items are a Specialty Product that should be used in unique areas.

●  Not recommended for high traffic areas.

●  Avoid high moisture/humidity areas. Cork is a natural product and is very porous. Moisture can cause     	mold or mildew and cause the edges of the cork squares to curl away from the backing.

●  When installing, any paste or water on the surface will stain.

●  Avoid prolonged exposure to direct sunlight.

●  The color of the cork may change slightly over time due to oxidation.

●  Do not crease. Cork will crack if tucked or wrapped into or around corners. Must cut cork at all corners 	when installing.

●  This is not a surface washable wallcovering.  To clean, wipe with a dry, lint-free cloth or vacuum.

3/2016